SECTION 02276

SEGMENTAL RETAINING WALL UNITS

Part 1 - general

1.1	Description

1.	Work Included:  Furnish and install segmental retaining wall (SRW) units to the lines and grades designated on the construction plans.

1.2	Related Work

1.	Related Sections:  Additional Sections of the Documents which are referenced in this Section include:

1)	Section 02300 - Earthwork

1.3	References

1.	General:  The work shall comply with the most recent standards or tentative standards as published at the date of the contract and as listed in this specification using the abbreviation shown.

2.	American Society for Testing and Materials (ASTM):

1)	C 90	Standard Specification for Loadbearing Concrete Masonry Units

2)	C 140	Standard Test Methods of Sampling and Testing Concrete Masonry Units

3)	D 698	Standard Test Method for Laboratory Compaction Characteristics of Soil Using Standard Effort (12,400 ft-lbf/ft3)

4)	D 1557	Standard Test Method for Laboratory Compaction Characteristics of Soil Using Modified Effort (56,000 ft-lbf/ft3) (2,700 kN-m/m3)

1.4	Certification

1.	General:  CONTRACTOR shall submit a notarized manufacturer's certification prior to start of work stating that the SRW units meet the requirements of this specification.

1.5	Delivery, Storage and Handling

1.	General:  CONTRACTOR shall check the materials upon delivery to assure that specified type, grade, color and texture of SRW units has been received.  CONTRACTOR shall prevent excessive mud, wet concrete, epoxies, and like materials which may affix themselves, from coming in contact with the materials.

2.	Damage:  CONTRACTOR shall protect the materials from damage.  Damaged material shall not be incorporated into the reinforced soil wall.

1.6	Measurement and Payment

1.	Measurement: of the SRW units is on a vertical square foot basis.

2.	Payment: shall cover supply and installation of SRW units along with appurtenant  and incidental materials required for construction of the retaining wall as shown on the construction plans.  It shall include all compensation for labor, materials, supplies, equipment and permits associated with building these walls.

3.	Quantity: of retaining wall as shown on plans may be increased or decreased at the direction of the OWNER based on construction procedures and actual site conditions.

PART 2 - MATERIALS

2.1	Segmental Retaining Wall Units

1.	Segmental Retaining Wall: units shall be VERSA-LOK Retaining Wall Units.

2.	Architectural Requirements:  SRW units shall meet the following Architectural requirements:

1) 	Color of SRW units shall be determined by OWNER.

2)	Finish of SRW units shall be split face.

3)	SRW unit faces shall be of straight geometry.

4)	SRW unit shall have a maximum height of 6 inches

5)	SRW units shall be capable of being erected with a variable bond configuration.  Bond should vary between ¼ to ¾ bond.

6)	All SRW units shall be sound and free of cracks or other defects that would interfere with the proper placing of the unit or significantly impair the strength or permanence of the construction.  Cracking or excessive chipping may be grounds for rejection.  Units showing cracks larger that ½ inch when measured along their length shall not be used within the wall. Units showing chips visible at a distance of 30 feet from the wall shall not be used within the wall.

3.	Structural Requirements:  SRW units shall meet the following structural requirements:

1)	The SRW units shall be solid through the full depth of the unit.

2)	For constructability considerations, the SRW units shall provide a minimum weight of 125 psf of wall face area.

3)	Concrete used to manufacture SRW units shall have a minimum 28 days compressive strength of 3000 psi in accordance with ASTM C 90 and C 140. The concrete shall have adequate freeze/thaw protection with a maximum moisture absorption rate, by weight of 8 percent.  Compressive strength test specimens shall conform to the saw-cut coupon provisions of Section 5.2.4 of ASTM C 140 with the following exception:  Coupon shall be taken from the least dimension of the unit of a size and shape representing the geometry of the unit as a whole.

4)	SRW units molded dimensions shall not differ more than +/- 1/8 inch from that specified, except height which shall be +/- 1/16 inch.

4.	Constructability and Geometric Requirements:  SRW units shall meet the following constructability and geometric requirements:

1)	Units shall be capable of attaining concave and convex curves and 90 to 140 degrees inside corners and 25 to 90 degree outside corners.

2)	Units shall be positively engaged to the unit below with connection pins so as to provide a 3/4 inch horizontal setback per 6 inch-high course (a cant of 7 degrees from vertical).  The installed wall cant shall not differ more than + or - 2 degrees from that specified.

2.2	Segmental Retaining Wall Unit Connection Pins

1.	General:  SRW connection pins which interlock the units shall meet all SRW manufacturer's specifications.

2.3	Leveling Pad

1.	Material: for leveling pad shall consist of compacted sand or gravel and shall be a minimum of 6 inches in depth.  The leveling pad should extend laterally at least a distance of 6 inches beyond the toe and heel of the lower most SRW unit.

2.	Mechanical Vibrations:  Do not run mechanical vibrating plate compactors on top of the units.  Compact fill between units by running hand-operated compaction equipment just behind unit.  Compact to minimum 95 percent Standard Proctor Density (ASTM D 698) or 90 percent of Modified Proctor Density (ASTM D 1557).

2.4	Drainage Aggregate

1.	Drainage Fill Materials: shall be the free draining gravel per manufacturer’s specifications.

2.	Vertical Drainage: layer behind the wall face shall be placed no less than 1 foot 3 per 1 foot 2 of wall face.

2.5	Reinforced Backfill (Infill Soil)

1.	Reinforced Backfill Material:  The reinforced backfill material shall be free of debris and consist of either of the following inorganic soil types according to their USCS designations (GP, GW, SW, SP, SM, ML, CL).  The maximum particle size shall be 4 inches.  There shall be less than 20 percent by eight of particles greater than 1½ inches, maximum 60 percent by weight passing the #200 sieve and PI<20.

2.	Backfill Compaction:  The reinforced backfill shall be compacted in maximum 8 inch-thick compacted lifts to a minimum density of 95 percent of maximum density as measured by ASTM D 698.

2.6	Retained Backfill or Common Backfill

1.	Soil:   Soil placed behind the reinforced backfill can be any inorganic soil with a liquid limit less than 50 and plasticity index less than 30, or as directed by the OWNER.

2.	Retained Backfill: shall be compacted to a minimum 95 percent of maximum density as determined by ASTM D 698.

PART 3 - EXECUTION

3.1	Excavation

1.	General:  CONTRACTOR shall excavate to the lines and grades shown on the project grading plans.  CONTRACTOR shall take precautions to minimize over-excavation.  Over-excavation shall be filled with compacted infill material, at the CONTRACTOR's expense.

3.2	Leveling Pad Construction

1.	General:  Leveling pad shall be placed as shown on the construction plans with a minimum thickness of 6 inches.  The leveling pad should extend laterally at least a distance of 6 inches from the toe and heel of the lower most SRW Unit.

3.3	SRW Unit Installation

1.	General:  First course of SRW units shall be placed on the leveling pad.  The units shall be leveled side-to-side, front-to-rear and with adjacent units and aligned.  The first course is the most important to ensure accurate and acceptable results.  Insure that units are in full contact with base.

1)	Place the front of the units side-by-side.  Do not leave gaps between the front of adjacent units.  Alignment may be done by means of a string line or offset from base line to the back of the units or along the pinning grooves.  Lay out of curves and corners in accordance with SRW manufacturer's installation guidelines.

3.	Placement and Compaction:  Place and compact drainage fill between and behind units.  Place and compact infill soil behind drainage fill.

4.	Debris:  Clean all excess debris from top of units and install next course.

5.	Connection Pun Insert:  Insert two connection pins for each unit through pin holes of the upper course units into receiving slots in lower course unit.  Pins shall be fully seated in the pin slot below.  Push units forward to remove any looseness in the unit-to-unit connection and then check alignment.  Check level of the units.

6.	Procedures:  Repeat procedures to the extent of the wall height, ensuring that pins are engaged in each successive course.

7.	SRW caps shall be glued to underlying units with manufacturer's recommended concrete adhesive.  Caps shall (overhang, be flush with, or be setback from) the top course of units.

END OF SECTION